ORFIT

Classic remains the ideal product for those who have used it over many years and appreciated its qualities.

®

With a bit of skill and experience, it is by far the most convenient basic material. It can be used to produce the simplest or most sophisticated splints, which are aesthetically pleasing to look at and ensure high performance.

The excellent adhesive qualities of ORFIT

®

Classic ensure that your splint adheres reliably and for a long time - no other thermoplastic can offer such performance. Without any glue or technical solvents, you simply attach hook and loop tape, springs, joints or ORFITUBES.

Less experienced users can simply follow the practical tips to adjust or reduce adhesion, such as: • Add liquid antiseptic to the water in the heating vessel •Wet the patient’s limbs to prevent

Classic from sticking to skin or hair • Put hand cream on the patient’s limbs.

ORFIT

®

Classic adheres accidentally or deliberately, you can remove it again whenever you require, simply by heating it in water. You can then use it again.

But regardless of whether ORFIT

ORFIT

Classic Soft ORFIT

®

®

Classic Stiff

®

Both materials have precisely the same degree of rigidity at room temperature (i.e. when it is “cold”).

The difference can be seen in the level of elasticity achieved when they are heated and the way in which they fit into the contours of the body.

Classic Soft is ideal for: • Small and average-sized splints and • Maximum precision in following the anatomical contours.

ORFIT

®

ORFIT

Classic Stiff is ideal for: • Larger splints or • Applications where the strength of the elastic memory is important for effective moulding to the anatomy.

®

ORFIT Soft

O